Jones Environmental Laboratory	CEN 10:1 LEACHATE RESULTS PrEN 12547-2

| Mass of sample taken (kg) - Moisture Content Ratio (%) = 16.4 Mass of dry sample (kg) = 0.09 Dry Matter Content Ratio (%) = 85.9 Particle Size <4mm = >95% |
| --- |
| JEFL Job No |  | Landfill Waste Acceptance Criteria Limits |
| Sample No |  |  |
| Client Sample No |  | Inert Waste Landfill | Stable Non-reactive Hazardous Waste in Non-Hazardous Landfill | Hazardous Waste Landfill |
| Depth/Other |  |  |  |  |
| Sample Date |  |  |  |  |
| Batch No |  |  |  |  |
| Solid Waste Analysis |  |  |  |  |
| Total Organic Carbon (%) |  |  | 3 | 5 | 6 |
| Loss on Ignition (%) |  |  |  |  | 10 |
| Sum of BTEX (mg/kg) |  |  | 6 |  |  |
| Sum of 7 PCBs (mg/kg) |  |  | 1 |  |  |
| Mineral Oil (mg/kg) |  |  | 500 |  |  |
| PAH Sum of 17(mg/kg) |  |  | 100 |  |  |
| pH (pH Units) |  |  |  | >6 | - . |
| ANC to pH 7 (mol/kg) |  |  | - | to be evaluated 1 |
| ANC to pH 4 (mol/kg) 1 |  |  | - |  |
| Eluate Analysis | 10:1 concn leached |  | Limit values for compliance leaching test using BS EN 12457-2 at L/S 10 I/kg |
|  | C10 |  |  |  |
|  | mg/I |  |  | mg/kg |
| Arsenic |  |  |  | 0.5 | 2 | 25 |
| Barium |  |  |  | 20 | 100 | 300 |
| Cadmium |  |  |  | 0.04 | 1 | 5 |
| Chromium |  |  |  | 0.5 | 10 | 70 |
| Copper |  |  |  | 2 | 50 | 100 |
| Mercury |  |  |  | 0.01 | 0.2 | 2 |
| Molybdenum |  |  |  | 0.5 | 10 | 30 |
| Nickel |  |  |  | 0.4 | 10 | 40 . |
| Lead |  |  |  | 0.5 | 10 | 50 |
| Antimony |  |  |  | 0.06 | 0.7 | 5 |
| Selenium |  |  |  | 0.1 | 0.5 | 7 |
| Zinc |  |  |  | 4 | 50 | 200 |
| Chloride |  |  |  | 800 | 15000 | 25000 |
| Fluoride |  |  |  | 10 | 150 | 500 |
| Sulphate as SO4 |  |  |  | 1000 | 20000 | 50000 |
| Total Dissolved Solids |  |  |  | 4000 | 60000 | 100000 |
| Phenol |  |  |  | 1 |  |  |
| Dissolved Organic Carbon |  |  |  | 500 | 800 | 1000 |